Dip Tank Cleaner / Metal Striper

General Product Information

Cautionary Measures

For an extensive list of precautionary measures and emergency

Product Number C ommon Name Application

AC- ACDTCSM

Metal Strip SM Dip Tank Cleaner

Metal Cleaner (Soft)

procedures, refer to the MSDS.

Personal protective equipment recommended for handling and use

Description 	 This alkaline powdered dip tank cleaner, is designed for removing rust, carbonized soils and paint. It may be used in a variety of applications

and industries to clean heavy equipment, remove rust and clean metal prior to painting or plating. For use on soft/fine metals.

Directions

Add product to a partially filled container of cold water. Do not add to hot water. Gradually increase temperature after adding. The

Gloves Respirator Eyewear Footwear Clothing Other

Impermeable gloves required. Dust mask required.

Chemical goggles or face shield required. Rubber boots required.

Impermeable coveralls required.

Eye-wash station and shower required.

recommended concentration is 3 - 8% at a temperature of 80 - 90 °C. Contact time may vary from 30 minutes to 8 hours. When removed from dip tank rinse thoroughly with fresh water.

Packaging Availability

This product is available in the following packaging options:

10 Kg	20 Kg	50 Kg	150 Kg

Physical Properties

For an extensive list of physical properties, refer to the MSDS.

General first-aid and emergency measures

In case of inhalation

Remove victim to fresh air. If breathing is difficult, oxygen may be beneficial if administered by trained personnel. Immediately transport victim to an emergency care facility.

In case of Ingestion 	 DO NOT INDUCE VOMITING. Have victim drink large amounts of water. Seek medical attention.

In case of contact with skin

In case of contact with skin, remove contaminated clothing and flush

with water for at least 60 minutes. Do not interrupt flushing. Transport

State

O   dour

C   olor

Specific Gravity pH

Powder

Odourless White n.av.

12.5 ± 0.5

to an emergency facility.

In case of contact with eyes

In case of contact with eyes, continuously flush eyes with plenty of water or neutral saline solution for at least 60 minutes. Transport to emergency facility.

General handling procedures and storage requirements

Handling procedures

Due to the toxic and corrosive nature of this product, it is important that adequate PPE and personal hygiene requirements are met.

Storage Requirements

Store in a cool, dry place. Keep containers tightly closed when not in use. Prolonged storage may cause this hygroscopic product to become wet and encrusted due to atmospheric moisture. Protect from damage.

Preparation of TDS

For further details on the source of this information, see MSDS.

Prepared by

Released

Altachem Ltd.

01/01/2010

Altachem Ltd.

4111-98th Street NW Edmonton, AB. T5E 5N5

1-866-414-1445

Page 1 of 1